## Slide 1: Summer Industrial Internship
ABHINAV AZAD |ED17B001
Tsujido,
Japan
SAIMA CORPORATION

## Slide 2: Content:
Objective
Material Study
Market Research
Basics of Torque Analyzer
Experiment Data & Plots
Results, Tends & Conclusion

## Slide 3: Objectives:
To understand Hard Plastic Market.
To check workability of the New Special Non-sert for Bakelite and Epoxy.
Investigate and find suitable conditions(Drill Hole & Load) for the Special Non-sert screw.

## Slide 4: Hard Plastics ~ Thermoset Plastics
A Thermosetting plastic is a polymer that irreversibly becomes rigid when heated.
Brittle, which makes machining tough on it.
Highly Resistive towards Heat and Electricity
Hence, well-suited to the production of permanent components and large, solid shapes.
Major Focus on:
BAKELITE
EPOXY Resin

## Slide 5: Bakelite- Market Research
BAKLITE transformed the lives of people as it was discovered:
Replaced skins, bone, ivory, wood, metals, plant fibers, and animal hair.
It is Heat and Chemical resistant, so used extensive in Industries as insulator and resistors.
Jewelry, clocks, radios, telephones, kitchenware, tableware, playing tools.

## Slide 6: Major types :
Paper Bakelite
Excellent mechanical strength, High impact strength
USES: Where mechanical strength is more important than electric insulation- wear resistance, resilience.
Potential Market: Electric Boards, Electronic Industry, Fashion industry.
Disadvantages: Water Absorption over long period usage.
Manufacturers/dealers: Shreelam Insukation(Mumbai), INSULECT, ZTELEC Group, SUMITOMO BAKELITE, Krishna Hylam
Fabric Bakelite
High impact strength, Good Machinability, Non-abrasive, Chemically resistant.
USES: Electrical Isolating Bolt Sleeves, Washers and Gaskets, Wear plates, Gears, roller, spacers
Potential Market: Textile Shuttles, pickers, Gears, Pulley, Bearing & wearing Plate.
Disadvantages: Water Absorption over long period usage,
Manufacturers/dealers: SUMITOMO BAKELITE, INSULECT, Krishna Hylam

## Slide 7: Properties Comparison:
Paper Bakelite
Parameters | Paper based | Fabric based
Density | 1.3-1.4 g/cc | 1.4- 1.5g/cc
Composition | Cellulose pulp + phenolic resin | Woven Cotton Fabric+phenolic resin
Colour | Black/Orange | Brown/ Natural
Price rate | 57 yuan/kg | 19 yuan/kg.
Heat Resistance | 140 C | 125 C
Flexural Strength | 130 MPA | 110MPA
Water Absorption (D-24/23, thickness 1.6mm) | 265 mg | 220 mg
Fabric Bakelite

## Slide 8: Bakelite- Market Research
automotive industry in the Asia-Pacific region.
North America and European in aerospace and power generation industries

## Slide 9
Bakelite- Market Research
Bakelite is a 3-D cross-linked network structured thermosetting polymer which is difficult to recycle after use.
Bakelite is proved to be hazardous to the atmosphere during production processes such as compilation, manufacturing, and dumping.
These factors are expected to hinder the market growth over the foreseeable future.

## Slide 10: It is seen that Bakelite resin has been replaced by epoxy resin in recent times with more reinforcement features embedded in them.
Compared tensile strength matrices, epoxy has higher value than Bakelite too.

## Slide 11: EPOXY- Market Research
Low water Absorption, Excels in insulation and heat resistance.
USES: manufacture of spacers, mechanical barriers, Insulation Plate, Permanent long-term installments.
Potential Market: Electronics Industries, Navy, Housing Solutions.
Disadvantages: Poor machinability (causes cracks)
Manufacturers/dealers: Nan Ya Plastic Corporation (Taiwan), Olin (U.S), Kukdo Chemical co limited (Japan),Aditya Birla Chemicals Ltd RISHO, CARBEX, FR4 Materials

## Slide 12: Properties ~ EPOXY :
Parameters | EPOXY
Density | 1.8g/cc
Composition | Bonded with glass fiber cloth and epoxy resin
Colour | White, Green
Price rate | 23 and 43 yuan/kg
Heat Resistance | 140-160 C
Flexural Strength | 130 MPA
Water Absorption | 0.10%

## Slide 13: EPOXY- Market Research
The global epoxy resin market size was USD 7.99 billion in 2015.
North America is another dominant region in the global market, exhibiting an expanding CAGR (Compound Annual Growth Rate).
Increased R&D coupled with technology advancement in the field of modified resins is expected to create new avenues for industrial applications.
Notes: https://www.grandviewresearch.com/industry-analysis/epoxy-resins-market (source)

## Slide 14: TORQUE ANALYZER
To understand and develop latest fastening technology, Torque analyzer helps arriving at quicker and efficient results.
Measures resistive Torque Vs Time for any given Rotational Speed(PRM).
Parameters used in a Torque Analyzer:
RPM
Fastening Bit
LOAD

## Slide 15: Normal Idling
When a fastening is successful, which means all the parameters compliments well enough for a workable screw tightening, its usually called Normal Idling

## Slide 16: CAM-OUT
Unsuccessful Fastening.
The Drill bit comes out of the hole, loosing the connection between with screw.
Head Break
Successful Fastening.
Screw Top breaks apart from the screw body.

## Slide 17
Normal Idling
Head Break
CAM OUT
PLOTS Comparison

## Slide 18: FASTENERS for PLASTICS
Conventional Fasteners which requires Inserts
Dealer: NYLTITE Corporation of America

## Slide 19: Do we have a Better way?

## Slide 20: Self-Tapping screws: INSERT NOT NEEDED!
Cost reduction, No Thread Insert Required
Faster to Install
Robust Application
More Efficient and less Failure
Sophisticated Manufacturing.
Forms Female Thread part on its own as it screws in the Hole

## Slide 21: Fasteners for Thermoset Plastics
Brittle Material
Much Harder than Thermoplastics
Limited and Selective Market.
CHALLENGES:

## Slide 22: Delta PT-S
Everything same as Delta PT with addition of Shank Slot at the end.
Multi-compound 30° flank angle and root for dynamic safety
Increased vibrational safety by improved pitch
Cutting edge for lower installation torque

## Slide 23: SAIMA’s Special NONSERT
Thread Angle: 30 Degrees Pitch : 1.1mm Thread Profile: Triangular
Cutting EDGE (Slank Shot)
NONSERT: A brand of SAIMA that features Self-Tapping screws.
Special NONSERT: NONSERT screws specially meant for Thermoset plastics

## Slide 24: The Design:
Reduces stress due to low flank angle.
Insert elimination possible.
Offers Repeatability in thermosets.
The special Triangular thread profile such that the material can exert resistance only at the three edges unlike in the circular one, where resistance is at all the points of the thread line.

## Slide 25: Testifying SAIMA’s Special Non-sert for Thermoset Plastics
Results and Analysis of Torque Analyzer Outputs upon testing the screws on different loads and implications.

## Slide 26: Bakelite Material

## Slide 27
3.7 MM BIT Material: Brown Paper Bakelite (NO CAM OUTS) |  |  |  |  | 
Load | 181 N | 151 N | 131 N | 111 N | 91N
TD | 0.712 | 0.588 | 0.656 | 0.687 | 0.588
TS | 2.48 | 2.06 | 2.28 | 2.51 | 2.06
TF | 4.27 | 3.562 | 3.919 | 4.353 | 3.562
F/D | 6.011 | 6.05 | 5.97 | 6.336 | 6.054
3.6 MM BIT Material: Brown Paper Bakelite (5/12 CAM OUTS) |  |  |  |  | 
Load | 181 N | 151 N | 131 N | 111 N | 91N
TD | 0.682 | 0.734 | 0.721 | 0.759 | 0.728
TS | 2.67 | 2.80 | 2.45 | 2.77 | 3.26
TF | 4.7 | 4.894 | 4.194 | 4.807 | 5.804
F/D | 6.962 | 6.67 | 5.82 | 6.32 | 8.205
3.5 MM BIT Material: Brown Paper Bakelite (5/12 CAM OUTS) |  |  |  |  | 
Load | 181 N | 151 N | 131 N | 111 N | 91N
TD | 0.710 | 0.739 | 0.728 | 0.731 | 0.665
TS | 2.78 | 2.4 | 2.52 | 2.43 | 2.34
TF | 4.787 | 4.084 | 4.331 | 4.141 | 4.038
F/D | 6.92 | 5.52 | 5.95 | 5.66 | 6.126

## Slide 28
Chart: TS Trends (Brown Paper Bakelite)
| 3.7mm | 3.6mm | 3.5mm
181 N | 2.48 | 2.67 | 2.78
151 N | 2.06 | 2.8 | 2.4
131N | 2.28 | 2.45 | 2.52
111N | 2.51 | 2.77 | 2.43
91N | 2.06 | 3.26 | 2.34
Chart: TD Trends (Brown Paper Bakelite)
| 3.7mm | 3.6mm | 3.5mm
181 N | 0.712 | 0.682 | 0.71
151 N | 0.588 | 0.734 | 0.739
131N | 0.656 | 0.721 | 0.728
111N | 0.687 | 0.759 | 0.731
91N | 0.588 | 0.728 | 0.665
Chart: TF Trends (Brown Paper Bakelite)
| 3.7mm | 3.6mm | 3.5mm
181 N | 4.27 | 4.7 | 4.787
151 N | 3.562 | 4.894 | 4.084
131N | 3.919 | 4.194 | 4.331
111N | 4.353 | 4.807 | 4.141
91N | 3.562 | 5.804 | 4.038
Chart: F/D Trends (Brown Paper Bakelite)
| 3.7mm | 3.6mm | 3.5mm
181 N | 6.011 | 6.962 | 6.92
151 N | 6.05 | 6.67 | 5.52
131N | 5.97 | 5.82 | 5.95
111N | 6.336 | 6.32 | 5.66
91N | 6.054 | 8.205 | 6.126
CAM OUT

## Slide 29: Drill Bit: 3.5/3.6/3.7 mm Load: 181/151/131/111/91 Newtons
As Load Increases all the Plots appears o shift UPWARDS, until failure(CAM OUT) is observed.
Cam out was observed for loads lesser than 111 N. We can also notice an Unusual Bump in the plots.
For 91 N some of the testing were successful but others were failing (CAM-OUT).
And, for 71 N all the test samples failed, except 3.7mm samples(1/12 failed), which also shows that for a larger Hole, Failure and Driving Torque decreases.
No Head Breaking observed as now.
With cumulative Observation 131N Load working most CONSISTENT and hence, reliable which is used in further testing.
RESULTS

## Slide 30: Load: 131 Newtons | Drill Bit: 3.6 mm | Nos: 36 holes
Material | TD |  |  | TS | TF |  |  | F/D |  | 
 | MIN | AVG | MAX |  | MIN | AVG | MAX | MIN | AVG | MAX
Brown Paper Bakelite | 0.65 | 0.721 | 0.81 | 2.45 | 3.96 | 4.12 | 4.32 | 5.11 | 5.836 | 6.55
Black Paper Bakelite | 0.61 | 0.731 | 0.89 | 2.58 | 4.11 | 4.45 | 4.87 | 5.10 | 6.128 | 7.41
Fabric Bakelite | 0.81 | 0.941 | 1.17 | 2.88 | 4.41 | 4.85 | 5.3 | 4.1 | 5.185 | 6.02
Chart: Trends over 3 Materials under 131 N load(3.6mm drill Holes)
| TD.min | TD.avg | TD.max | TS | TF.min | TF.avg | TF.max | F/D.avg
Brown Paper Bakelite | 0.65 | 0.72 | 0.81 | 2.45 | 3.96 | 4.12 | 4.32 | 5.836
Black Paper Bakelite | 0.61 | 0.731 | 0.89 | 2.58 | 4.11 | 4.45 | 4.87 | 6.128
Fabric Bakelite | 0.81 | 0.941 | 1.17 | 2.88 | 4.41 | 4.85 | 5.3 | 5.185
Chart: Trends over Material under 131 N load(3.6mm drill Holes)
| Brown Paper Bakelite | Black Paper Bakelite | Fabric Bakelite
TD.min | 0.65 | 0.61 | 0.81
TD.avg | 0.72 | 0.731 | 0.941
TD.max | 0.81 | 0.89 | 1.17
TS | 2.45 | 2.58 | 2.88
TF.min | 3.96 | 4.11 | 4.41
TF.avg | 4.12 | 4.45 | 4.85
TF.max | 4.32 | 4.87 | 5.3
F/D.avg | 5.836 | 6.128 | 5.185

## Slide 31: Load: 131 Newtons | Drill Bit: 3.7 mm | Nos: 24 holes
Material | TD |  |  | TS | TF |  |  | F/D |  | 
 | MIN | AVG | MAX | 2.19 | MIN | AVG | MAX | MIN | AVG | MAX
Brown Paper Bakelite | 0.58 | 0.654 | 0.72 |  | 3.57 | 3.705 | 3.79 | 5.21 | 5.7 | 6.47
Black Paper Bakelite | 0.60 | 0.704 | 0.77 | 2.34 | 3.58 | 4.00 | 4.41 | 4.90 | 5.708 | 6.50
Fabric Bakelite | 0.73 | 0.846 | 0.97 | 2.23 | 3.36 | 3.641 | 3.92 | 3.56 | 4.331 | 5.05
Chart: Trends over 3 Materials under 131 N load(3.6mm drill Holes)
| TD.min | TD.avg | TD.max | TS | TF.min | TF.avg | TF.max | F/D.avg
Brown Paper Bakelite | 0.58 | 0.654 | 0.72 | 2.19 | 3.57 | 3.705 | 3.79 | 5.7
Black Paper Bakelite | 0.6 | 0.704 | 0.77 | 2.34 | 3.58 | 4 | 4.41 | 5.708
Fabric Bakelite | 0.73 | 0.846 | 0.97 | 2.23 | 3.36 | 3.641 | 3.92 | 4.331
Chart: Trends over Material under 131 N load(3.7mm drill Holes)
| Brown Paper Bakelite | Black Paper Bakelite | Fabric Bakelite
TD.min | 0.58 | 0.6 | 0.73
TD.avg | 0.654 | 0.704 | 0.846
TD.max | 0.72 | 0.77 | 0.97
TS | 2.19 | 2.34 | 2.23
TF.min | 3.57 | 3.58 | 3.36
TF.avg | 3.705 | 4 | 3.641
TF.max | 3.79 | 4.41 | 3.92
F/D.avg | 5.7 | 5.708 | 4.331

## Slide 32
Chart: Trends over Material under 131 N load (3.6mm drill Holes)
| TD.min | TD.avg | TD.max | TS | TF.min | TF.avg | TF.max | F/D.avg
Brown Paper Bakelite | 0.65 | 0.72 | 0.81 | 2.45 | 3.96 | 4.12 | 4.32 | 5.836
Black Paper Bakelite | 0.61 | 0.731 | 0.89 | 2.58 | 4.11 | 4.45 | 4.87 | 6.128
Fabric Bakelite | 0.81 | 0.941 | 1.17 | 2.88 | 4.41 | 4.85 | 5.3 | 5.185
Chart: Trends over Material under 131 N load(3.6mm drill Holes)
| Brown Paper Bakelite | Black Paper Bakelite | Fabric Bakelite
TD.min | 0.65 | 0.61 | 0.81
TD.avg | 0.72 | 0.731 | 0.941
TD.max | 0.81 | 0.89 | 1.17
TS | 2.45 | 2.58 | 2.88
TF.min | 3.96 | 4.11 | 4.41
TF.avg | 4.12 | 4.45 | 4.85
TF.max | 4.32 | 4.87 | 5.3
F/D.avg | 5.836 | 6.128 | 5.185
Chart: Trends over Material under 131 N load (3.7mm drill Holes)
| TD.min | TD.avg | TD.max | TS | TF.min | TF.avg | TF.max | F/D.avg
Brown Paper Bakelite | 0.58 | 0.654 | 0.72 | 2.19 | 3.57 | 3.705 | 3.79 | 5.7
Black Paper Bakelite | 0.6 | 0.704 | 0.77 | 2.34 | 3.58 | 4 | 4.41 | 5.708
Fabric Bakelite | 0.73 | 0.846 | 0.97 | 2.23 | 3.36 | 3.641 | 3.92 | 4.331
Chart: Trends over Material under 131 N load(3.7mm drill Holes)
| Brown Paper Bakelite | Black Paper Bakelite | Fabric Bakelite
TD.min | 0.58 | 0.6 | 0.73
TD.avg | 0.654 | 0.704 | 0.846
TD.max | 0.72 | 0.77 | 0.97
TS | 2.19 | 2.34 | 2.23
TF.min | 3.57 | 3.58 | 3.36
TF.avg | 3.705 | 4 | 3.641
TF.max | 3.79 | 4.41 | 3.92
F/D.avg | 5.7 | 5.708 | 4.331

## Slide 33
Load: 131 Newtons | Drill Bit: 3.7 mm VS 3.6 mm
Material |  | TD |  |  | TS | TF |  |  | F/D |  | 
 |  | MIN | AVG | MAX |  | MIN | AVG | MAX | MIN | AVG | MAX
Brown Paper Bakelite | 3.6mm | 0.65 | 0.72 | 0.81 | 2.45 | 3.96 | 4.12 | 4.32 | 5.11 | 5.836 | 6.55
 | 3.7mm | 0.58 | 0.654 | 0.72 | 2.19 | 3.57 | 3.705 | 3.79 | 5.21 | 5.7 | 6.47
Black Paper Bakelite | 3.6mm | 0.61 | 0.731 | 0.89 | 2.58 | 4.11 | 4.45 | 4.87 | 5.10 | 6.128 | 7.41
 | 3.7mm | 0.60 | 0.704 | 0.77 | 2.34 | 3.58 | 4.00 | 4.41 | 4.90 | 5.708 | 6.50
Brown Fabric Bakelite | 3.6mm | 0.81 | 0.941 | 1.17 | 2.88 | 4.41 | 4.85 | 5.3 | 4.1 | 5.185 | 6.02
 | 3.7mm | 0.73 | 0.846 | 0.97 | 2.23 | 3.36 | 3.641 | 3.92 | 3.56 | 4.331 | 5.05
Comparing the previous two Samplings
MAX

## Slide 34
For Paper Bakelite (Brown/Black), 3.6 drill bit is providing a better result in our testing.
TD is always lower in 3.6mm Holes.
But TF and F/D for 3.7 and 3.6 drill bit are showing considerable difference.
Hence overall, 3.6 drill holes ore optimum for both Paper and Fabric Bakelite with a load of 131 N.
For Fabric Bakelite, the TD Values are highest which means Fabric Bakelite needs a higher driving Torque than other. Also because it is much tougher and stronger due to various reinforcements.
Load: 131 Newtons | Drill Bit: 3.7 mm VS 3.6 mm
RESULTS

## Slide 35: Epoxy Material

## Slide 36: Load: 131 Newtons | Drill Bit: 3.7/3.6 mm | Nos: 24 holes
Material/ Specs | TD |  |  | TS | TF |  |  | F/D |  | 
 | MIN | AVG | MAX |  | MIN | AVG | MAX | MIN | AVG | MAX
Epoxy3.6mm (9/24 CAM OUTS) | 0.72 | 0.906 | 1.07 | 3.43 | 5.26 | 5.81 | 6.43 | 5.04 | 6.52 | 8.3
Epoxy 3.7mm (3/24 CAMOUTS) | 0.72 | 0.838 | 1.1 | 2.8 | 4.53 | 4.9 | 5.54 | 4.27 | 5.9 | 7.0

## Slide 37
For the 3.6 mm hole fastening, 9/24 cam-out occurred, 4/24 head breaks occurred and overall 13/24 samples failed i.e. more than 50 percent samples were unsuccessful.
Torque vs Time plots for the head break samples were unique and understandable.
For 3.7 mm hole fastening, 3/24 cam-out occurred and other were successful with good performance data.
High Driving Torque (TD) Values are observed
Load: 131 Newtons | Drill Bit: 3.7/3.6 mm | Nos: 24 holes
RESULTS

## Slide 38: Suggestions / Hypothesis:
3.6 mm drill holes are not suitable for the given Tapping screws in epoxy material.
3.7 mm drill holes can be deployed.
We can have further testing on 3.7 mm drill holes with higher torque to avoid Cam-out instances.

## Slide 39: Load: 151/141 Newtons | Drill Bit: 3.7 | Nos: 24 holes
Material/ Load | TD |  |  | TS | TF |  |  | F/D |  | 
 | MIN | AVG | MAX |  | MIN | AVG | MAX | MIN | AVG | MAX
Epoxy 3.7, 131 N (3/24 CAMOUTS) | 0.72 | 0.838 | 1.1 | 2.8 | 4.53 | 4.9 | 5.54 | 4.27 | 5.9 | 7.0
Epoxy 3.7, 141 N (NO CAMOUTS) | 0.69 | 0.82 | 0.97 | 2.4 | 3.74 | 4.2 | 4.67 | 4.02 | 5.16 | 6.67
Epoxy 3.7, 151 N | 0.63 | 0.838 | 0.98 | 2.55 | 3.45 | 3.98 | 4.55 | 3.67 | 4.98 | 6.46

## Slide 40: Load: 151/141/131 Newtons | Drill Bit: 3.7 | Nos: 24 holes
For a Load of 131 Newtons there were 3 Camouts/ 24 tests. But just by a difference of 10 N load, there was a great improvement in performance and No Camouts were observed.
Although TF values are lowered on increasing Load but TD values are also decreased. And overall, it’s not a problem.
Best optimum results are shown in 141 N Load, which is also an affordable load for manual fastening, because for 141 Newtons there is no risk of Camouts which are there in 131 N load.
On further higher load (151 N) performance turns bad.
RESULTS

## Slide 41: In Bakelite(Paper and Fabric) using 3.6mm drill holes with 131 Newton load is most reliable.
In epoxy using 3.7mm drill holes with 141 Newton load is most reliable.
Final Conclusions:

## Slide 42: Conclusive Trends:
Driving Torque decreases with increase in hole diameter.
CAM OUTS happening for lesser Loads and smaller Diameter holes. ----------------------------------------------------------------
Failure Torque decreases with increase in hole diameter.
Head Breaks happening at much Higher Loads and smaller Diameter Holes.

## Slide 43: SAIMA’s Outreach in India

## Slide 44: Centre for Innovation, IIT Madras, India
A Large student community in IIT Madras, working towards innovation.

## Slide 45: Competition Teams
RAFTAAR: Student formula race Car team
ANVESHAK: Conquest of building best Mars Rover
Notes: http://cfi.iitm.ac.in/wordpress/

## Slide 46: RAFTAAR, Student formula team
Notes: http://cfi.iitm.ac.in/raftar/views/sponsors.html

## Slide 47: ANVESHAK, manipulator robot team
Competing in International Mars Rover Competitions
Notes: https://www.youtube.com/watch?v=VEyJ4maBrkg#action=share
http://www.anveshak.team/

## Slide 48: Aarigato Gozaimasta ありがとうございました
Thankyou!